## Slide 1
Project Flexible, Biocompatible, and Wirelessly Powered Implantable Optoelectronics | What I did last four weeks? Design final version of the circuit. Write Paper for IEEE Sensors Canada. Write Paper for IEEE Circ. Italy Write report. Prepare devices and automatize. production of the implants.
Problem being faced? Paper writing. Experiments. | What to do in next two weeks? Write Report. Prepare experimental data. Analyse the experimental data.
Gabriel Galeote Checa

## Slide 2: Bioimplantable Device
Final Version of the Circuit
1. Current work
Antenna tuned for 13.56 MHz
Antenna tuned for 8 MHz

## Slide 3: Bioimplantable Device
1. Current work
5mm
2cm

## Slide 4: Bioimplantable Device
1. Current work
Main Considerations for Fabrication
Soldering technique using reflow oven: need for control of the especific ammount of solder paste

## Slide 5: Bioimplantable Device
2. Fabrication Results Verification

## Slide 6: Bioimplantable Device
2. Fabrication Results Verification
POLYIMIDE
COPPER
COPPER-POLYIMIDE BONDING

## Slide 7: Bioimplantable Device
2. Fabrication Results Verification
Problems of the fabrication:
  Bonding Copper-Polyimide very inestable
  Copper strength decreases after reflow oven  It gets more rigid.
  With a bigger size of the copper trace, greater stability.

## Slide 8: Bioimplantable Device
3. Experimental Results
Test of the 8 MHz and 13.56 MHz.
This experimental results proofs:
The usefulness of the modular design giving us the option of changing the antena easily while keeping same electrical properties.
The correct operation of the Voltage regulator showin the stable voltaje within the bandwidth.
The limitation of the máximum power of the shank proving the effectivity of the voltaje regulator.

## Slide 9: Bioimplantable Device
3. Experimental Results

## Slide 10: Bioimplantable Device
3. Experimental Results
The effect of the protection resistance for the LED:
  Higher resistance, longer distance.
  The operation of the LED in respect to the distance is not linear, PROOF of the Voltage Regulator effect on the circuit.

## Slide 11: Bioimplantable Device
Further Steps
Finish IEEE Cir. And Elec. Syst.
Prepare Poster for MSc Thesis
Write MSc Thesis

## Slide 12: Bioimplantable Device
Thank for the attention